## Slide 1: 3D synthetic microstructure generation involving grain size, shape and orientation representation
Sheila Lizardi Schad
Aalto University
Mondragon university
08.07.2021
Professor
Juhne Lian

## Slide 2: Index
RVE generation
  Workflow
  Grain shape control
  Evaluation
Further developments
  Post-process
  Grain shape aspect ratio evaluation
  Grain axis orientation control
Final RVE
RVE with other filters
  Variant grain shape aspect ratio
  Variant grain axis orientation
Conclusions and outlook
Grain size
Grain shape
Grain orientation
Misorientation angle
Orientation of crystal lattice

## Slide 3: RVE generation – Workflow
Microstructure characterization
Grain size / shape / orientation distribution figures
Representativeness of RVE  MRAC / MRAD
Δ=mean
[1] W. Liu, J. Lian, N. Aravas, and S. Münstermann, “A strategy for synthetic microstructure generation and crystal plasticity parameter calibration of fine-grain-structured dual-phase steel,” Int. J. Plast., vol. 126, no. October 2019, p. 102614, 2020, doi: 10.1016/j.ijplas.2019.10.002.

## Slide 4: RVE generation – Grain shape control
Three different approaches
  Equiaxed
  Average method  Mean values
  Grain shape distribution  Fitting parameters of beta distribution 
Optimal numerical parameter  Mesh size
RVE uncertainty 10 parallel RVE generations
 | Shape distribution a | Shape distribution b (RD-TD) | Shape distribution c (RD-ND) | Alpha parameter | Beta parameter
Equiaxed | 1 | 1 | 1 | - | -
Average method | 1 | 0.74 | 0.72 | - | -
Grain shape distribution | - | - | - | 4.73 | 1.62

## Slide 5: RVE generation – Grain shape control
Taking any grain shape control method it can be seen how the mesh size does not affect much on results
The best approach is the beta distribution method  Gets the closest to experimetal results
Microstructure representative assessment criterion
Best approach  Shape distribution
Grain size error  very small in all three cases
The texture index error  Best with shape distribution
 |  | Grain size | Grain shape asp. Ratio | ODF error | Texture index | Δ, % | Grain number
Approach | Equiaxed | 0.0005 | 0.23 | 0.92 | 0.27 | 2.38 | 2705
 | Mean values | 0.0026 | 0.04 | 0.97 | 0.29 | 1.82 | 2693
 | Shape distribution | 0.0010 | 0.0103 | 0.72 | 0.15 | 1.11 | 2697

## Slide 6: Evaluation – Mesh size
Mesh size, μm | Grain size | Grain shape asp. ratio | ODF error | Texture index | Δ, % | Grain number
5 | 0.01 | 0.0002 | 1.60 | 1.52 | 4.7 | 378
10 | 0.0010 | 0.0103 | 0.72 | 0.15 | 1.11 | 2697
15 | 0.05 | 0.0119 | 0.82 | 0.47 | 4.12 | 7832
20 | 0.15 | 0.015 | 0.80 | 0.53 | 4.33 | 15694
Comparation of exp. data and output for:
Grain size Orientation

## Slide 7: Further development – Post-process
Using DREAM3D and MATLAB/MTEX
1. Procedure grain
Do analysis of each 2D plane
Remove edge grains and one size pixels
Create final RVE and analyze with data from all layers
Data from generated ideal ellipsoid seeds
Data overlapping, and does not fulfill the whole 3D space
2. Final grain morphology
3D
2D
[2] Generating Synthtic Microstructures w/DREAM3D: An overview Tutorial, The Air Force research laboratory

## Slide 8: Further development – Grain shape aspect ratio control
Big improvement in grain shape aspect ratio results

## Slide 9: Further development – Grain axis orientation control
Grain axis orientation: orientation between the RD axis and the longest axis of the fitted ellipse.
For control in DREAM3D
  Input for every 15 degrees
  Depending on the density  Higher or lower input values
  Strong orientation  Small standard deviation values for input
The analysis of the orientation is done with MATLAB/MTEX
0º
90º

## Slide 10: Final RVE
Mesh size, μm | RVE size, |  | Grain number |  |  | 
10 | 64x64x64 |  | 2538 |  |  | 
 | Grain size, mm |  | Grain shape aspect ratio |  | t | ODF error
 | µ | σ | α | β |  | 
Input | 3.56 | 0.58 | 4.73 | 1.62 | 2.5362 | 0.5573
RVE | 3.05 | 0.43 | 5.53 | 0.62 | 3.2283 | 
Mesh size, μm |  |  | Grain number |  |  | 
10 | 64x64x64 |  | 2538 |  |  | 
 | Grain size, mm |  | Grain shape aspect ratio |  | t | ODF error
 | µ | σ | α | β |  | 
Input | 3.56 | 0.58 | 4.73 | 1.62 | 2.5362 | 0.5573
RVE | 3.05 | 0.43 | 5.53 | 0.62 | 3.2283 | 
RD
TD
ND

## Slide 11: RVE with variant grain shape control
Input of grain shape aspect ratio of:
Very elongated Nearly equiaxed
1:0.1:0.1 1:0.9:0.9

## Slide 12: RVE with variant tilt angle control
45º
90º
180º

## Slide 13: Conclusions and outlook
Conclusions
MRAC  Good method to evaluate RVE
Shape control method ( Grain shape distribution method)
  Very good control of grain shape (Grain shape aspect ratio and axis orientation)
Optimal RVE with optimal mesh size
Modification of postprocess for grain shape from 3D to 2D
Control of size, shape and orientation distribution
Outlook
Control misorientation

## Slide 14
Contact info.:
Email: Sheila.lizardischad@aalto.fi
Sheila.lizardi@alumni.mondragon.edu